# The effects of whey protein molecular weight (MW) on film water vapor permeability (WVP), mechanical properties and solubility at three plasticizer levels were studied.  Both 5.5% and 10% degree of hydrolysis (DH) whey protein isolate (WPI) had significant difference (p<0.05) on film tensile properties and solubility compared to unhydrolyzed WPI.  Little or no significant difference (p>0.05) appeared for film WVP between unhydrolyzed WPI, 5.5% DH WPI and 10% DH WPI films. Thus, use of hydrolyzed WPI increased film flexibility without need for additional glycerol (gly) and without increasing WVP.  Increase in gly content significantly increased film WVP and elongation, and decreased elastic modulus and maximum strength before break.  Soluble Protein (SP) and total soluble matter (TSM) of hydrolyzed WPI films were much higher than for unhydrolyzed WPI films.

Edible films and coatings have shown potential for controlling transfer of moisture, oxygen, lipid, aroma and flavor compounds in food systems, with resulting increase in food quality and shelf life (Donhowe and Fennema, 1993; Krochta, 1997a; Krochta and De Mulder-Johnston, 1997b).  However, much research is still needed to better understand the effect of film structure on film properties.

Whey protein has been shown to make transparent films with good oxygen, aroma and oil barrier properties (McHugh et al., 1994; Mate and Krochta, 1996; Mate and Krochta, 1996; Miller, 1997; De Mulder-Johnston, 1999).  However, such films are quite brittle due to extensive intermolecular forces involving protein chain-to-chain interaction.  One approach to overcome such film brittleness is addition of food grade plasticizers to the film  formulation.  Plasticizers reduce intermolecular forces along the whey protein polymer chains, with resulting increase in the mobility of polymer chains and more flexible films (Banker, 1966).  Another possible approach to reducing intermolecular forces along polymer chains is to reduce polymer molecular weight, with resulting increase in polymer chain end groups and polymer free volume (Sears and Darby, 1982).  This may decrease the amount of added plasticizer in films; consequently, it may minimize permeability of films while producing needed film flexibility. Hydrolyzed WPI also reduces the allergenicity of milk protein, which is attributable to the globular nature of the protein (Nielsen, 1997).

The objective of this study was to determine the effect of reduction of whey protein molecular weight on film WVP and mechanical properties to achieve desirable films. Additionally, the effect of whey protein molecular weight on film solubility was determined.

# Molecular Weight Effects

WVP.  WVP of WPI films was slightly different from that of 10% DH WPI films (p<0.05) at 25% gly content, as shown in Fig.1.  However, there was no significant difference between WVP of WPI and 5.5% DH WPI films (p>0.05).  Furthermore, there was no significant difference found between unhydrolyzed WPI, 5.5% DH WPI and 10% DH WPI film WVP at 30 and 35% gly content.  These results are consistent with the results of Perez-Gago et al. (1999) on WVP between native and denatured WPI films and the results of Mate and Krochta (1996) on WVP between WPI and (-lactoglobulin films, which showed that whey protein composition and structure had no effect on WVP.  Thus, effect of WPI hydrolysis on film WVP does not have the same trend as added plasticizer.

Mechanical Properties.  Type of WPI had a significant effect on film elastic modulus, maximum strength and % elongation (p<0.05), as shown in Figs. 2, 3 and 4.  Hydrolyzed WPI films were more flexible (lower elastic modulus), weaker, and had smaller elongation than WPI at the same gly contents.  Extent of MW reduction cannot explain this situation, since 10%DH WPI has smaller MW than 5.5%DH.  The difference may be attributable to differences in the hydrolysis process for the two materials.

Solubility.  Solubility is an important protein functional property.  Generally, protein solubility increases with an increase in DH, because of the reduction of protein MW resulting in increase of the number of polar groups.  The same trend was found for WPI films.  WP MW had a significant effect on  % TSM and % SP (p<0.05), as shown in Figs. 5 and 6.  WPI films maintained their integrity in water, whereas 5.5%DH WPI films completely dissolved. The 10%DH WPI films maintained their integrity during immersion contrasted with 5.5%DH WPI films which completely dissolved.  This is consistent with the finding that 10%DH WPI films were stronger and had larger elastic modulus than 5.5%DH WPI films. The 10%DH WPI films gave higher % TSM than WPI films, but less than that of 5.5%DH WPI films.  This might be due to the different enzyme, pH, treatment condition, etc. used to produce the two different hydrolyzed WPI products.  The 5.5%DH WPI gave the highest % SP (64-75%) following by 10%DH WPI films (30-34%) and WPI films (2.8-3.2%).  These results are consistent with the % TSM results.  Hydrolyzed WPI has increased solubility because the reduction of peptide bonds increases the NH3+ and COO- content in the protein (Nielsen, 1997).  Thus, changes in properties due to hydrolysis of peptide bonds include decrease in MW, destruction of globular protein structure, and increase in solubility.

Hydrolyzed WPI makes good films with larger solubility than WPI films. This study showed that the use of hydrolyzed WPI can reduce the gly content required to impart desired film flexibility and can minimize WVP of WPI films. Since hydrolyzed WPI reduces the allergenicity of milk protein, hydrolyzed WPI coatings may be acceptable on nuts and fruit for allergic people.

Banker, G. S. 1966. Film coating theory and practice. J. Pharm. Sci. 55(1): 81-89.

De Mulder-Johnston, C. 1999.  Thermal analysis of, and oil migration through films from, whey protein isolate.  Ph.D. Dissertation, Univ. of California, Davis.

Donhowe, G. and Fennema, O. 1993. Water vapor and oxygen permeability of wax films. JAOCS 70(9): 867-873.

Krochta, J. M. 1997a. Edible protein films and coatings. In Food Proteins and Their Applications, S. Damodaran and A. Paraf (Ed.), p. 529-549. Marcel Dekker, Inc., New York.

Krochta, J. M. and De Mulder-Johnston, C. 1997b. Edible and biodegradable polymer films: challenges and opportunities. Food Technology, 51:61-74.

Mate, J. I. and Krochta, J. M. 1996. Comparison of oxygen and water vapor permeabilities of whey protein isolate and b-lactoglobulin edible films. J. Agric. Food Chem. 44(10): 3001-3004.

McHugh, T.H., Avena-Bustillas, R., and Krochta, J.M. 1993.  Hydrophilic edible films: modified procedure for water vapor permeability and explanation of thickness effects.  J. Food Sci. 58(4): 899-903.

McHugh, T. H., Aujard, J. F., and Krochta, J.M. 1994. Plasticized whey protein edible films: water vapor permeability properties. J. Food Sci. 59(2): 416-419, 423.

Miller, K.S. and Krochta, J.M. 1997.  Oxygen and aroma barrier properties of edible films: A review.  Trends in Food Science and Technology. 8: 228-237.

Nielsen, P. M. 1997. Functionality of protein hydrolysates. In Food Proteins and Their Applications, S. Damodaran and A. Paraf (Ed.), p.443-472. Marcel Dekker, Inc., New York.